# COLOUR

Light grey and dark grey with nuances.

# Product description

The bricks are formed individually in the unsanded mould to a solid mass, pressed from clay of alluvial origin from an area located in the Scheldt basin and fired in a tunnel oven at a temperature of approximately 1180°C. On the narrow side the bricks have an unsanded surface structure.  The shape is slightly irregular. Finally the bricks are processed until they have acquired a weathered
shape, due to which the paver surface leaves a rustic, aged impression.  The brick is fired a second time with complete reduction.

# TECHNICAL CHARACTERISTICS

The paving is laid in fired clay bricks of Belgian origin, quality class A, carrying the Benor mark, the CE mark and UKCA mark.

CE label according to EN 1344 : 2013 / AC : 2015

| Manufacturing dimensions (L x W x H) | *212x51x104 mm | on demand for projects > 2000 m² |
| --- | --- | --- |
| Quantity / m² with a traditional joint | ca. 91 |  |
| Manufacturing dimensions (L x W x H) | *212x69x104 mm | on demand for projects > 2000 m² |
| Quantity / m² with a traditional joint | ca. 68 |  |

# PHYSICAL AND MECHANICAL PROPERTIES ACCORDING TO EN 1344: 2013 / AC: 2015

| Aspect | Class | Mean | Individual |
| --- | --- | --- | --- |
| Water absorption NBN EN771 | Class W3 | max 3% | max 4% |
| Transverse breaking load NBN EN1344 | Class T4 | min 80 N/mm | min 64 N/mm |
| Abrasion resistance NBN EN1344 | Class A3 | max 450 mm³ | max 500 mm³ |
| Frost resistance NBN EN1344 | Class FP100 | freeze/thaw resistant | freeze/thaw resistant |
| Size tolerance NBN EN1344 | Class R1 | ± 0,4 √d | 0,6 √d (range) |
| Wet skid resistance NBN EN1344 | Class U3 | >55 |  |
| Acid resistance NBN EN1344 | Klasse C | < 7% | < 7% |

# Productshot