# COLOUR

Purple

# Product description

The bricks are formed individually in the sanded mould to a solid mass, pressed from clay of alluvial origin from an area located in the Scheldt basin and fired in a tunnel oven at a temperature of approximately 1180°C. On the narrow side the bricks have an sanded surface structure.

# TECHNICAL CHARACTERISTICS

The paving is laid in fired clay bricks of Belgian origin, quality class A, carrying the Benor mark, the CE mark and UKCA mark.

CE label according to EN 1344 : 2013 / AC : 2015

| Manufacturing dimensions (L x W x H) | *217x52x70 mm |  |
| --- | --- | --- |
| Quantity / m² with a traditional joint | ca. 85 |  |

# PHYSICAL AND MECHANICAL PROPERTIES ACCORDING TO EN 1344: 2013 / AC: 2015

| Aspect | Class | Mean | Individual |
| --- | --- | --- | --- |
| Water absorption NBN EN771 | W3 | Max 3% | Max 4% |
| Transverse breaking load | T4 | Min 80 N/mm | Min 64 N/mm |
| Abrasion resistance | A3 | Max 450 mm³ | Max 500 mm³ |
| Frost resistance | FP100 | freeze/thaw resistant | freeze/thaw resistant |
| Wet skid resistance | U3 | >55 |  |
| Acid resistance | C | < 7% |  |
| Size tolerance | R1 | Max. ± 0,4 √d | Max. 0,6 √d |

# Productshot